青岛光大国贸

QINGDAO EVER BRIGHT TRADING CO. LTD

No.17, Shanghai Rd, Qingdao Free Trade Port Zone

17号，上海路，青岛保税港区 Huangdao, Qingdao, China 黄岛，青岛，中国

MU-86

Product description:  Sulfited fish oil

Chemical properties:

Appearance:        Brownish liquid

PH(10%):           6.0-8.0

Charge:            Anionic

Activity:           85±2％

Leather properties:

※Good penetrating and evening

※Perfect softness and roundness.

※Improve strength and tearing effect

Application:

- Applied on soft leathers like Garment, Nappa、Nubuck and upholstery etc.

Storage:

The appearance of MU-86 will change at different temperature. It will be paste below 5℃ and becomes to orange mash below 15℃. When the temperature is higher than 25℃, MU-86 will be transparent brownish liquid. The quality is not affected by these changes.

Stir well before use.